CERTIFICATE OF ANALYSIS

Date issued October 20, 2010











   Version: 2.0


	Trade name
	AO 565 DD

	Chemical name
	2,6-di-tert-butyl-4-(4,6-bis(octylthio)-1,3,5-triazin-2-ylamino) phenol

	Structure
	



	CAS No.
	991-84-4

	Molecular weight
	589 g/mol

	Batch No.
	565101507

	Manufacturing date
	October 15, 2010

	Expiration date
	October 15, 2012

	Test item
	Specifications
	Test results

	Appearance
	white to yellowish pellets
	white pellets

	Specific Gravity (20˚C):
	1.09 g/cm3
	1.09 g/cm3

	Assay(HPLC)
	>99%
	99.3%

	Transmittance(425nm)

(5% w/w in toluene)
	>=95%
	96.4%

	Transmittance(500nm)

(5% w/w in toluene)
	>98%
	99.1%

	TGA Test (weight loss)
	1.0% max at 268˚C 

10.0% max at 328˚C 
	0.75%

8.6%

	Ash content
	<0.1%
	0.02%

	Storage
	At least 2 years when stored in cool and dry conditions, in the original sealed containers

	Hazards
	According to the present state of knowledge provided that this product is handled correctly there is no known danger to humans. 
Please observe the safety regulations in the Safety Data sheet.



